## Slide 1: Resonant Soft X-ray Spectroscopy on

## Slide 2
Trilayers of rocksalt Cu(II)O are sandwiched between planes of Cu(I)
The Lithium randomly substitutes the Cu(II) ions
Lattice: tetragonal crystal structure (P4/mmm, a = 2.81 A ̊, c = 8.90 A ̊)

## Slide 3: RIXS
Strong core hole – electron coulomb interaction, causes exciton generation (dd exciation)

## Slide 4: Wave polarisation
LV
LH

## Slide 5: RIXS results

## Slide 6: RSXS result

## Slide 7: RIXS results – normalized along the peak

## Slide 8: Fitting Spectrum with lorentzian Curve

## Slide 9: Fitting Spectrum with lorentzian Curve

## Slide 10: Fitting Spectrum with lorentzian Curve

## Slide 11: Fitting Spectrum with lorentzian Curve
Bragg condition

## Slide 12: Fitting Spectrum with lorentzian Curve
Bragg condition

## Slide 13: Resonance Frequencies
Polarization | L3 edge |  | L2 edge | 
LCP | 937.9 | 940.9 | 958 | 961.15
LV(960) | 938.05 | 941.05 | 958.15 | 961
RCP(1324) | 938.05 | 941.05 | 958.15 | 961.15
LH | 937.9 | 940.9 | 958.3 | 961.3
RCP(2057) | 938.15 | 941.05 | 958.15 | 961.15
LV(2595) | 938.2 | 941.2 | 958.2 | 961.3
Polarization | L3 edge |  | L2 edge | 
LCP | 937.9 | 940.9 | 958 | 961.15
LV(960) | 938.05 | 941.05 | 958.15 | 961
RCP(1324) | 938.05 | 941.05 | 958.15 | 961.15
LH | 937.9 | 940.9 | 958.3 | 961.3
RCP(2057) | 938.15 | 941.05 | 958.15 | 961.15
LV(2595) | 938.2 | 941.2 | 958.2 | 961.3
Differences due to not sufficiently small enough Energy steps??
Difference from theory – about 6eV ??

## Slide 14: Extracting physical quantities from fit data
Lorentzian curve: .
According to [Seve,2]:
With d being the lattice constant in the [001] direction.
FWHM~
Thus:

## Slide 15: Extracting physical quantities from fit data
Lorentzian curve: .
According to [Seve,2]:
With d being the lattice constant in the [001] direction.
FWHM~
Thus:

## Slide 16: Extracting physical quantities from fit data
Lorentzian curve: .
According to [Seve,2]:
With d being the lattice constant in the [001] direction.
FWHM~
Thus:

## Slide 17: Unrealistic oscilations

## Slide 18: Unrealistic oscilations
Fitting gold 4f edge for obtaining reference oscilations

## Slide 19: Unrealistic oscilations
Fitting gold 4f edge for obtaining reference oscilations
Transforming data from fit to relative scattering angle as:

## Slide 20: Unrealistic oscilations
Fitting gold 4f edge for obtaining reference oscilations
Transforming data from fit to relative scattering angle as:
Smoothing data of peak position as a reference for the chi-square test to obtain best fit

## Slide 21: Unrealistic oscilations
Fitting gold 4f edge for obtaining reference oscilations
Transforming data from fit to relative scattering angle as:
Smoothing data of peak position as a reference for the chi-square test to obtain best fit
Using the test substracting reference oscilations to minimize oscilating behaviour
unwiggling

## Slide 22: Unrealistic oscilations
Fitting gold 4f edge for obtaining reference oscilations
Transforming data from fit to relative scattering angle as:
Smoothing data of peak position as a reference for the chi-square test to obtain best fit
Using the test substracting reference oscilations to minimize oscilating behaviour
unwiggling

## Slide 23: Dielectric Tensor

## Slide 24: Kramers Kronig Analysis

## Slide 25: Kramers Kronig Analysis

## Slide 26: Kramers Kronig Analysis
SOLUTION?

## Slide 27: Kramers Kronig Analysis
SOLUTION?

## Slide 28: Kramers Kronig Analysis for Imaginary part

## Slide 29: Kramers Kronig Analysis for Imaginary part

## Slide 30: Total Electron Yield

## Slide 31: Circular Magnetic X-ray Dichroism (CMXD)

## Slide 32: Optical Conductivity

## Slide 33: Optical Conductivity

## Slide 34: Reference
[1] X-ray Circular Dichroism as a Probe of Orbital Magnetization, B-T. Thole, Paolo Carra, F. Sette and G. van der Laan
[2] Determination of the Anomalous Scattering Factors in the Soft-X-ray Range using Diffraction from a Multilayer, L. Seve, J. M. Tonnerre and D. Raoux
[3] Theory of Resonant Inelastic X-Ray Scattering by Collective Magnetic Excitations, M.W. Haverkort
[4] Kramers–Kronig Relations in Optical Materials Research, V. Lucarini, J.J. Saarinen, K.-E. Peiponen, E.M. Vartiainen
[5] Angle-Resolved Photoemission Spectroscopy of Tetragonal CuO: Evidence for Intralayer Coupling Between Cupratelike Sublattices – Supplementary Information, S. Moser